SOME Crystal CIF INFORMATION:

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

?

;

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'As4 Na4 Se8'

_chemical_formula_weight          1023.32

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'Na'  'Na'   0.0362   0.0249

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'As'  'As'   0.0499   2.0058

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Se'  'Se'  -0.0929   2.2259

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_symmetry_cell_setting            monoclinic

_symmetry_space_group_name_H-M    pc

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'x, -y, z+1/2'

_cell_length_a                    11.682(2)

_cell_length_b                    5.9021(7)

_cell_length_c                    11.8231(19)

_cell_angle_alpha                 90.00

_cell_angle_beta                  90.446(13)

_cell_angle_gamma                 90.00

_cell_volume                      815.2(2)

_cell_formula_units_Z             2

_cell_measurement_temperature     100

_cell_measurement_reflns_used     5842

_cell_measurement_theta_min       3.45

_cell_measurement_theta_max       29.18

PWSCF INPUT

&control

prefix='gamma-NaAsSe2,

outdir="/tmp"

pseudo_dir='/opt/PWscf-4.0.5/pseudo/'

calculation='scf'

disk_io     = "high",

nstep       = 100,

restart_mode = "from_scratch”

/

&system

ibrav=12,

A=11.682,

B=5.9021,

C=11.8231,

COS(AB)=0

COS(AC)=-0.0078

COS(BC)=0

nat=32,

ntyp=3,

ecutwfc=25,

/

&ELECTRONS

electron_maxstep = 500,

diago_david_ndim = 6,

mixing_beta = 0.3,

/

ATOMIC_SPECIES

Na  22.99   Na.pbe-n-van.UPF

As  74.92   As.pbe-n-van.UPF

Se  78.96   Se.pbe-van.UPF

ATOMIC_POSITIONS angstrom

As                 8.69727171    5.49957678    9.16640817

As                 0.01114570    5.34789281    0.00886706

As                 2.84243931    3.22018576   11.39357627

As                 5.74343300    5.85783425   11.19814635

Se                11.18136503    5.75513771    9.46233140

Se                 2.60689267    3.06200948    9.07229915

Se                 5.32855366    3.49758446   11.65497710

Se                 5.71392187    5.84780068    2.96857224

Se                 8.19121530    5.76694191   11.55152810

Se                 2.37962456    5.60581458   11.76540150

Se                11.52385714    2.86901081    6.10384514

Se                 8.47246873    3.18064169    8.91659364

Na                11.40481486    2.80172687    9.04557975

Na                 2.75550537    5.79055031    2.88711355

Na                 5.52920263    3.00475911    8.68971522

Na                 8.62039040    3.11394796    5.97166688

As                 8.74328775    0.40252322    3.25503727

As                -0.03487034    0.55420719    5.92023796

As                 2.88845535    2.68191424    5.48220537

As                 5.78944904    0.04426575    5.28677545

Se                11.22738107    0.14696229    3.55096050

Se                 2.65290871    2.84009052    3.16092825

Se                 5.37456970    2.40451554    5.74360619

Se                 5.66790583    0.05429932    8.87994314

Se                 8.23723134    0.13515809    5.64015720

Se                 2.42564060    0.29628542    5.85403060

Se                11.56987318    3.03308919    0.19247424

Se                 8.51848477    2.72145831    3.00522274

Na                11.45083090    3.10037313    3.13420885

Na                 2.70948933    0.11154969    8.79848445

Na                 5.57521866    2.89734089    2.77834432

Na                 8.66640644    2.78815204    0.06029598

K_POINTS automatic

1 1 1   0 0 0